## Slide 1
Materials Overview 1/2
Material Composition: Sustainable & High-Performance
9 / 39
Three building blocks — skeleton, function, and bonding — combine biodegradability with high performance.
🌿
Cellulose Derivatives
Plant-based biopolymers
Plant-derived biopolymers that form the backbone of the gel network.
3 types
HEC, MC, MHEC
Bio.
Highly biodegradable
Role
Viscosity & structure
◎
Colloidal Silica (CSP)
Colloidal Silica Particles
The key component that interacts dynamically with polymers and forms aerogel under heat.
Size
~22 nm monodisperse
Sinter
Forms silica skeleton
Role
Source of aerogel
⬡
PP Interaction
Polymer–Particle Interaction
Builds the network via dynamic, multivalent hydrogen bonds — no covalent bonds required.
Bonds
Dynamic H-bonds
Self-heal
Gel recovers after strain
Sprayable
Easy spray application

## Slide 2
Materials Overview 2/2
Mechanism: Spray, Adhesion, and Flame Protection
10 / 39
Not temperature, but shear and self-healing govern the spray-to-adhesion behavior.
01
At rest
Gel
High-viscosity elastic gel. G' > G'' holds structure.
Yield stress ~33 Pa
→
02
Spraying
Sol-like
Shear strain lowers viscosity; the gel flows.
Shear-thinning n < 1
→
03
On wall
Self-healing gel
Strain release instantly restores the gel network.
G' recovery ~90%
→
04
Flame
Aerogel
CSP sinters into a porous silica layer.
Acts as thermal barrier
POINT
Rather than relying on MC's thermal response (LCST), rheology alone achieves "spray → stick → set" — the core of this material.