## Slide 1
RESEARCH PRESENTATION · 2024
Adv. Mater. · Dong et al., 2024
WATER-ENHANCING GELS · ADVANCED MATERIALS 2024
Protecting Against
Heat-Activated Silica Aerogels
Next-generation fire-retardant gel of cellulosic polymers × colloidal silica particles
that self-foams upon heating to form an aerogel insulating layer
Materials Chemistry / Fire Protection Eng. · Stanford University, Appel Lab · Adv. Mater. 36, 2407375
DOI: 10.1002/adma.202407375
1 / 36

## Slide 2
Contents
Presentation Outline
2 / 36
●
PART 1
Background
Current state of wildfires, limitations of existing technologies (Phos-Chek, AquaGel-K), and innovation of this research
Slides 4–7
●
PART 2
Materials & Methods
Cellulosic polymers, CSP, formulations (5 types), evaluation methods
Slides 9–14
●
PART 3
Results
Rheology, combustion tests, foaming index, SEM observation, mechanism
Slides 16–33
●
PART 4
Discussion & Conclusion
Implementation scenarios, comparison with existing products, conclusions and future prospects
Slides 35–36
ⓘ
Key Message: Foaming upon heating + sintering of silica particles spontaneously forms an aerogel layer, achieving longer protection than commercial products

## Slide 3
01
Part 1
Background
Wildfire damage under climate change and the fundamental limitations of existing fire retardant technologies
Wildfire Status
Existing WEG / Retardants
Research Innovation
3 / 36

## Slide 4
Background 1/4
Growing Severity of Wildfire Damage and WUI Risk
4 / 36
5×
Increase in large-scale wildfires (past 30 years)
Driven by climate change and prolonged drought
45 million
U.S. WUI residents
High-risk population at the wildland–urban interface
Extended dry and high-wind seasons mean
conventional firefighting strategies can no longer keep pace
Image
(Paste paper figure here)
Wildfire / WUI boundary zone (photo)

## Slide 5
Background 2/4
Research Approach: 4-Stage Protection Process
5 / 36
Fig. 1a
(Paste paper figure here)
Gel application → flame contact → heat-activated aerogel formation → structural protection
1
Gel Application
Spray cellulosic gel
onto buildings and vegetation
2
Flame Contact
Moisture evaporates; gel
foams and particles aggregate
3
Aerogel Formation
Silica particles sinter into
a porous insulating layer
4
Sustained Protection
Ultra-low thermal conductivity
layer shields the substrate

## Slide 6
Background 3/4
Existing Wildfire Protection Methods and Their Fundamental Limitations
6 / 36
(photo)
Water only
H₂O
Runs off and evaporates
instantly — no persistence
(photo)
Phos-Chek
Ammonium phosphate
Chemical residue persists
in soil and water systems
(photo)
AquaGel-K
Cross-linked polyacrylate
Protection lost the moment
water evaporates
(photo)
WEG (This Work)
Cellulosic + Silica
Aerogel layer continues
protecting after water loss
Challenge: Existing WEGs are mere "water carriers" — protection vanishes the moment moisture is lost

## Slide 7
Background 4/4
Research Core: Heat-Activated Aerogel Formation
7 / 36
Heat-Activated
Aerogel Formation
Flame contact triggers the gel to transform into an aerogel insulator
01
Beyond water dependence
Heat-activated solid protective layer
02
Sustainable materials
Naturally derived, food-grade components
03
Drop-in compatible
Sprayable fluid — no new infrastructure needed
Concept
(Paste paper figure here)
Heat trigger transforms the gel into a porous aerogel insulating layer

## Slide 8
02
Part 2
Materials & Methods
Novel gel design combining cellulosic polymers and colloidal silica
Polymer Components
Silica Particles & Surfactant
Formulations (5 types)
Evaluation Methods
8 / 36

## Slide 9
Materials 1/6
Cellulosic Polymers Used
9 / 36
A
HEC
Hydroxyethyl cellulose
Base viscosity-building backbone
B
MC
Methyl cellulose
Gels on heating (thermoreversible) — key to flame protection
C
MHEC
Methyl 2-hydroxyethyl cellulose
Hybrid combining the traits of A and B
Fig. 1b/c
(Paste paper figure here)
Chemical structures and CSP mixing scheme

## Slide 10
Materials 2/6
Methyl Cellulose (MC) Thermal Gelation: Key Property for Flame Protection
10 / 36
THERMAL RESPONSE
Inverse Thermal Response (LCST Behavior)
•
MC dissolves in cold water (<20°C) to form a low-viscosity solution
•
Gelation above LCST upon heating
•
MC gelation onset: approx. 50–60°C (concentration-dependent)
•
Liquid at room temperature → instantaneous gelation upon flame contact
🔥
MC gelates in the initial stage of flame contact → maintains foamed structure while CSP is fixed
LCST (Gelation onset)
~55°C
1 wt% MC aqueous solution
Thermal decomposition
~300°C
TGA measurement
CSP sintering onset
~200°C
Inter-particle neck formation
Temperature-dependent Process
~55°C
MC gelation
Structure fixed
▶
~100°C
Moisture evaporation
Foaming & expansion
▶
~200°C
CSP sintering
Grain boundary formation
▶
>300°C
Organic decomposition
Pure silica layer

## Slide 11
Materials 3/6
Colloidal Silica Particles (CSP) and Surfactant (SDS)
11 / 36
●
CSP
Colloidal Silica Particles
•
LUDOX TM-50 (stock 50 wt%) → diluted to 15 wt% (pH 9)
•
Particle size: 22 nm (monodisperse)
•
Formulation concentration: 5 wt% in gel
•
Sinters upon heating → transforms into silica aerogel
◆
SDS (Additive)
Sodium Dodecyl Sulfate
•
Anionic surfactant
•
Adding SDS did not improve Foaming Index
•
Addition levels: two concentrations of 0.1 wt% and 0.5 wt%
•
Higher SDS concentration coarsens bubble size (SEM)
💡
The sintering temperature range of CSP overlaps with the thermal decomposition temperature of cellulose, enabling synchronized thermal response to form the insulating layer

## Slide 12
Materials 4/6
Five Formulations Evaluated
12 / 36
Control
AquaGel-K
0.5 wt%
Commercial WEG benchmark
Formula 1
HEC+MC / CSP
HEC+MC 1 wt%
CSP 5 wt%
Formula 2
MHEC / CSP
MHEC 1 wt%
CSP 5 wt%
Formula 3
HEC+MC / CSP / SDS
+ SDS 0.1 wt%
Formula 4
HEC+MC / CSP / SDS
+ SDS 0.5 wt%
Formulation Design Intent
•
Comparing functional differences by varying polymer type (HEC+MC vs MHEC)
•
Verifying the effect on foam structure with two SDS concentration levels
•
Direct comparison with commercial AquaGel-K
Notation Guide
HEC+MC/CSP/SDS 1-5-0.1
→ HEC+MC 1 wt% ／ CSP 5 wt% ／ SDS 0.1 wt%

## Slide 13
Materials 5/6
Overview of Evaluation Methods
13 / 36
RHEOLOGY
Rheological Measurements
•
Oscillatory frequency sweep (G', G'')
•
Steady-flow sweep (viscosity vs. shear rate)
•
Herschel-Bulkley model fitting
BURN TEST
Combustion Test (Time-to-char)
•
Whitewood plywood heated with MAP-Pro torch (~2054°C)
•
Time to charring onset measured
•
Photographic comparison at 120 s / 300 s
FOAMING
Foaming Index Measurement
•
Foamed layer thickness measured after combustion
•
Ratio to initial thickness = Foaming Index
SEM
SEM Morphological Observation
•
Foam structure by SDS concentration
•
Sintering progression by burn time (0/1/2/4 min)
SPECTROSCOPY
Spectroscopic Analysis
•
FT-IR (chemical bonding)
•
XPS (surface composition)
THERMAL
Thermal Analysis
•
TGA (thermogravimetric analysis)
•
DSC (differential scanning calorimetry)

## Slide 14
Materials 6/6
Adhesion and Surface Wettability: Properties Essential for Implementation
14 / 36
WETTING
Contact Angle Measurement
•
Contact angle evaluation on wood, concrete, and metal
•
WEG shows low contact angle → high wettability
•
HEC+MC shows particularly high affinity at cellulose-wood interface
ADHESION
Vertical Surface Adhesion Test
•
Gel applied to vertically oriented substrate
•
G' ≫ G'' → resists gravity without flowing down
•
Vertical surface retention equal to or better than AquaGel-K
SPRAY
Spray Application Suitability
•
Viscosity drops sharply under high shear (inside nozzle)
•
Quickly recovers high viscosity upon reaching substrate → maintains adhesion
•
Fully compatible with existing fire hoses and nozzles
✓
Rheological design (low n, high G') simultaneously achieves spray suitability and adhesion retention

## Slide 15
03
Part 3
Results
Rheological properties, combustion performance, foam structure, and aerogel formation mechanism
Rheology
Combustion Test
Foaming Index
SEM Observation
15 / 36

## Slide 16
Results 1/11
Rheology ①: Oscillatory Moduli G' / G''
16 / 36
Fig. 2a–b
(Paste paper figure here)
Angular frequency vs Storage modulus G' · Loss modulus G''
KEY OBSERVATION
Key Observation
•
G' > G'' for all formulations → solid-like (gel) behavior
•
Low frequency dependence → stable network
•
AquaGel-K (G'=457 Pa) shows higher G' than WEG (46/26 Pa); all formulations exhibit gel behavior
"
Clearly formed gel network; does not flow off after application

## Slide 17
Results 2/11
Rheology ②: Shear Thinning and Power-law Index
17 / 36
Fig. 2c–d
(Paste paper figure here)
Viscosity vs. shear rate (shear-thinning behavior)
Flow index n
n < 1
HEC+MC/CSP — strong shear thinning
Flow index n
n < 1
MHEC/CSP — shear thinning
n < 1 = shear-thinning
Lower values → better flow at high shear → excellent sprayability
💨
High viscosity at rest for adhesion, low viscosity during spraying — flow properties compatible with existing firefighting equipment

## Slide 18
Results 3/11
Rheology ③: Static Yield Stress and Long-term Stability
18 / 36
ƒ
Static yield stress: stress at the G'/G'' crossover (σ_s) from amplitude sweep — minimum stress to initiate flow
Formulation
Static yield stress (fresh)
Static yield stress (455 days)
Note
HEC+MC/CSP 1-5
33.34 Pa
68.9 Pa
Gel strength increases over time
MHEC/CSP 1-5
3.31 Pa
4.56 Pa
Long-term stability confirmed (455 days)
AquaGel-K (Commercial control)
—
—
Reference
Static Yield Stress
Measured at G'/G'' crossover from amplitude sweep. HEC+MC/CSP: 33.34 Pa; MHEC/CSP: 3.31 Pa (fresh)
Long-term Stability
MHEC/CSP shows only minor change after 455 days (3.31→4.56 Pa). Demonstrates shelf stability for practical use
HEC+MC vs MHEC
HEC+MC system shows ~10× higher yield stress, better for vertical surface adhesion. MHEC simpler to manufacture

## Slide 19
Results 4/11
Rheology ④: Storage Modulus G' and Viscoelasticity (tan δ)
19 / 36
G' Storage Modulus (1 rad/s)
MHEC/CSP 1-5
25.6 Pa
HEC+MC/CSP 1-5
46.4 Pa
AquaGel-K
456.8 Pa
ⓘ
All formulations show G'>G'' (gel behavior). AquaGel-K has the highest G' but also larger tan δ (more fluid-like)
Loss tangent tan δ = G''/G' (elastic-dominated = <1)
AquaGel-K
0.168
HEC+MC/CSP 1-5
0.219
MHEC/CSP 1-5
0.400
✓
All formulations: tan δ < 1 (gel behavior). AquaGel-K most elastic (0.168); MHEC system most fluid-like (0.400)

## Slide 20
Results 5/11
HEC+MC vs MHEC: Comparison of Two Systems
20 / 36
HEC + MC Mixed System
HEC (non-thermal gelation) + MC (thermal gelation, LCST)
•
HEC provides room-temperature viscosity and adhesion
•
MC maintains structure during heating
•
Strong shear thinning (n < 1)
•
Time to char > 7 min
•
Foaming Index ≈ 2.2–2.6
→ Good compatibility with SDS; excellent for optimizing foam structure
MHEC Single-Polymer System
MHEC (integrates HEC+MC functions into a single molecule)
•
Carries both hydroxyethyl and methyl groups on the same chain
•
Achieves equivalent viscoelasticity and thermal response with a single polymer
•
Shear thinning (n < 1)
•
Time to char > 5 min
•
Advantage of simplified formulation and quality control
→ Advantageous for scale-up and manufacturing cost reduction
⚖
Both systems significantly outperform commercial AquaGel-K. HEC+MC excels in foam optimization; MHEC excels in manufacturing simplicity

## Slide 21
Results 6/11
Combustion Test Setup
21 / 36
Fig. 3a
(Paste paper figure here)
Experimental setup for combustion testing
EXPERIMENTAL
◆ Test Conditions
•
Substrate: whitewood plywood
•
Gel application: uniformly applied
•
Flame source: MAP-Pro torch (~2054°C)
•
Measurement: time until substrate charring
•
Photographs taken at 120 s and 300 s
⏱
Time to char = time required for wood surface to char (longer = better protection)

## Slide 22
Results 7/11
Time to Char: Quantitative Comparison of 5 Formulations
22 / 36
Time to char (time to charring onset)
Water
~0.3 min
AquaGel-K (commercial)
~1.5 min
MHEC/CSP 1-5
>5 min
HEC+MC/CSP 1-5
>7 min
HEC+MC/CSP/SDS 1-5-0.1
>7 min
📊
This work's WEG achieves 3–6× longer protection than commercial AquaGel-K (n≥3 for all tests)
Fig. 3b
(Paste paper figure here)
Time-to-char bar chart (n≥3, error bars = standard deviation)

## Slide 23
Results 8/11
Time-lapse Observation of Combustion Process
23 / 36
Fig. 3c
(Paste paper figure here)
Sequential photographs during flame contact for each formulation
Water
•
Immediately evaporates and runs off under direct flame
•
Wood surface chars in ~0.3 min (~18 s)
•
No protective layer formed
AquaGel-K
•
Retains water but ends when water evaporates
•
Chars in ~1.5 min
•
No solid protective layer formed
This Work WEG
•
Gel foams and expands simultaneously with water evaporation
•
Porous aerogel layer provides continued protection
•
Charring prevented for >7 min (HEC+MC)

## Slide 24
Results 8/11
Surface Condition Comparison at 120 s / 300 s
24 / 36
Fig. 3d
(Paste paper figure here)
Surface condition comparison: 120 s (top) and 300 s (bottom)
Water
• 120 s: charring already beginning over wide area
• 300 s: entire surface blackened, severe damage
Time to char: ~0.3 min
AquaGel-K (commercial)
• 120 s: gel drying, partial charring
• 300 s: no protective layer, partial charring
Time to char: ~1.5 min
This Work WEG
• 120 s: aerogel layer forming and expanding
• 300 s: surface nearly intact, layer remains
Time to char: >7 min

## Slide 25
KEY RESULT
>7 min
Time to Char of This Work's WEG (HEC+MC/CSP)
Achieved 3–6× longer protection than commercial AquaGel-K (~1.5 min) — n≥3 for all tests
Water
~0.3 min
AquaGel-K
~1.5 min
This Work WEG
>7 min
25 / 36

## Slide 26
Results 9/11
Foaming Index Comparison
26 / 36
Fig. 4a
(Paste paper figure here)
Appearance of foamed layer after combustion
Fig. 4b
(Paste paper figure here)
Foaming Index for each formulation
Foaming Index (post-combustion thickness / initial thickness)
AquaGel-K
≈0
MHEC/CSP 1-5
≈2.1×
HEC+MC/CSP/SDS 1-5-0.1
≈2.3×
HEC+MC/CSP 1-5
≈2.6×
Insulating Effect from Foaming
•
Expands to >2× initial thickness → heat conduction path extended
•
Air trapped in pores enhances thermal insulation
•
AquaGel-K does not foam → collapses flat under flame
•
HEC+MC/CSP without SDS achieves the highest foaming index (≈2.6)

## Slide 27
Results 9/11
Effect of SDS Concentration on Aerogel Microstructure
27 / 36
Fig. 4c
(Paste paper figure here)
FE-SEM images by SDS concentration (0%, 0.1%, 0.5%)
0% SDS
Highest foaming index (≈2.6). No SDS yields maximum expansion.
0.1% SDS
Uniform fine-bubble structure. Foaming index ≈2.3 (lower than no-SDS).
0.5% SDS (Excess)
Non-uniform and coarsened bubble size. Foaming index further reduced.

## Slide 28
Results 10/11
FT-IR & XPS: Chemical Composition Changes (Before/After Combustion)
28 / 36
FT-IR Major Peak Assignments
Wavenumber (cm⁻¹)
Assignment
After combustion
3200–3500
O–H stretch (cellulose, water)
Disappears (dehydration)
2850–2950
C–H stretch (methyl groups)
Disappears (organic decomposition)
1050–1100
Si–O–Si stretch (silica)
Intensity increases
800
Si–O bending vibration
Becomes distinct
450
Si–O bending
Sharpens
🔥
Post-combustion spectrum matches pure silica (SiO₂) → aerogel formation chemically confirmed
XPS Surface Elemental Composition (at%)
Formulation
C 1s before (at%)
C 1s after (at%)
HEC+MC/CSP
25.6
14.9
MHEC/CSP
38.3
4.8
📊
Carbon greatly reduced (MHEC: 38.3→4.8 at%) → organic matrix combusted and removed; silica remains
Peak Position Verification
Si 2p peak: ~103.5 eV (consistent with SiO₂) / O 1s peak: ~533 eV

## Slide 29
Results 11/11
TGA/DSC: Thermal Decomposition Profile and Role of Each Component
29 / 36
TGA: Weight Loss Profile (N₂ atmosphere)
50–150°C: Evaporation of free and adsorbed water
200–350°C: Thermal decomposition of HEC/MC organic chains (main weight loss)
350–600°C: Oxidation and loss of residual carbon (in air)
>600°C: Silica residue (~5–8 wt%, no change)
DSC: Thermal Event Assignments
Temperature range
Event
ΔH
~100°C
Endothermic: water evaporation
Endothermic
~55–80°C
Exothermic: MC gelation transition
Slightly exothermic
~250–300°C
Exothermic: oxidative decomposition of organic chains
Exothermic
Final silica residue
~5–8 wt%
Equivalent to CSP 5 wt%
Cellulose decomposition peak
~280°C
Common to HEC/MC
🌡
CSP sintering (~200°C+) and cellulose decomposition (~280°C+) overlap in temperature → synchronized aerogel formation

## Slide 30
Supplementary 1/2
Mechanism of Silica Aerogel Formation
30 / 36
Fig. 5a
(Paste paper figure here)
3-stage schematic of WEG → silica aerogel transformation by flame activation
PHASE 1
Unsintered
•
Silica particles dispersed independently
•
Water fills the interstices
•
No inter-particle bonding
PHASE 2
Grain boundary
•
Particles approach as water evaporates
•
Grain boundaries form
•
Initial neck formation begins
PHASE 3
Necking & porosity
•
Necks grow and strengthen
•
Porosity decreases, skeleton complete
•
SiO₂ aerogel layer established

## Slide 31
Supplementary 2/2
Sintering Progression with Burn Time (SEM)
31 / 36
Fig. 5b
(Paste paper figure here)
Cross-section SEM images of HEC+MC/CSP 1-5 after 0, 1, 2, and 4 min heating
0 min
Unheated
•
Spherical particles dispersed independently
•
No inter-particle bonding
•
Water fills the matrix
1 min
Early sintering
•
Grain boundaries appear between particles
•
Initial necks form
•
Most moisture evaporated
2 min
Sintering in progress
•
Neck regions expand
•
Continuous network forms
•
Porosity decreasing
4 min
Aerogel complete
•
Dense SiO₂ skeleton complete
•
High mechanical strength
•
Functions as insulating layer

## Slide 32
04
Part 4
Discussion & Conclusion
Implementation scenarios, comprehensive comparison with existing products, research significance and future prospects
Implementation Scenarios
Performance Comparison
Summary
32 / 36

## Slide 33
Discussion 1/3
Implementation Scenarios: WEG Deployment Strategy
33 / 36
SCENARIO 1
Pre-protection of WUI Structures
•
Pre-applied to building exteriors and roofs before wildfire season
•
Can be applied by helicopter or ground hose
•
Protective function remains even after drying
SCENARIO 2
Protection of Critical Infrastructure
•
Power towers, substations, and communication base stations
•
Strongly adheres to metal structures as well
•
Prevents power outages and communication disruption
SCENARIO 3
Fire Break Formation
•
Pre-applied to vegetation along potential spread paths
•
No environmental burden unlike Phos-Chek
•
Cellulose and silica have low environmental persistence
Advantages Over Existing Methods
vs Water
Far greater protection (water chars at ~0.3 min)
vs AquaGel-K
3–6× longer protection + continues after water evaporation
vs Phos-Chek
No residual contamination in soil or water
Spray compatibility
Usable with existing equipment
🚁
Flow properties (shear thinning) compatible with both aerial and ground application are key to practical deployment

## Slide 34
Summary 1/2
Key Demonstrated Results
34 / 36
RHEOLOGY
Rheology
•
G' > G'', no crossover (gel)
•
G': HEC+MC≈46, MHEC≈26 Pa
•
Shear-thinning (HB) → sprayable
•
tan δ < 1, solid-like gel
FIRE PROTECTION
Fire Protection
•
HEC+MC/CSP: >7 min to char
•
MHEC/CSP: >5 min
•
3–6× more effective than commercial
•
Water ~0.3, AquaGel-K ~1.5 min
FOAMING / SEM
Foaming & Structure
•
Foaming Index up to ≈2.6
•
AquaGel-K does not foam (≈0)
•
Porous silica film on burning
•
Particles sinter after 2 min (SEM)
CHEMISTRY
Chemical Change
•
FT-IR: CH/SiO ratio drops
•
XPS: large carbon decrease
•
MHEC/CSP C 38.3%→4.8%
•
Silica (SiO₂) remains
◆
On burning, water evaporates while the gel converts into a porous silica aerogel — insulating the substrate even after desiccation (a mechanism absent in commercial WEGs)

## Slide 35
Summary 2/2
Conclusions
35 / 36
RESULT 01
●
3–6× more protective
HEC+MC/CSP >7 min, MHEC/CSP >5 min to char. Protects substrates far longer under flame
RESULT 02
●
Self-forming aerogel
Heat dehydrates the gel and sinters CSP → forms a porous silica aerogel insulating layer in situ (protection continues after drying)
RESULT 03
●
Compatible with spray infrastructure
Shear-thinning, sprayable fluid combining strong substrate adherence and wetting
RESULT 04
●
Sustainable, safe materials
Cellulose derivatives — Earth's most abundant biopolymer; biodegradability confirmed in prior study; silica is benign
Core Mechanism
•
Water rapidly evaporates on flame contact
•
CSP sinters, forming inter-particle necks
•
Porous silica aerogel insulating layer forms
Significance Stated in the Paper
•
PP platform as a basis for diverse fire retardants
•
Amenable to modular manufacturing & large scale
•
Fire retardancy retained after 455-day aging (MHEC/CSP)
"
From "water carrier" to "heat-self-transforming fire-retardant material" — a next-gen WEG that stays effective even after drying

## Slide 36
RESEARCH IMPACT
3–6×
Time to Char Improvement vs. Commercial WEG (AquaGel-K)
From "water carrier" to "self-transforming fire-retardant material"
The new WEG design paradigm opens a pathway to practical technology protecting critical infrastructure from wildfires
Time to char
>7 min
Foaming Index
≈2.6×
Shear-thinning
n < 1
36 / 36